PC-R20BK

Source   Sheet、Headlight Shell、CD        ， after cleaning granulation .

Application  Automotive、Drones

Performance table

|  | Testing standards |  |
| --- | --- | --- |
| Melt Flow Index | ASTM D1238 | 18-22 g/10min |
| Tensile strength | ASTM D638 | 60 MPa |
| Elongation | ASTM D638 | 45 % |
| Bending strength | ASTM D790 | 90 MPa |
| Bending modulus | ASTM D790 | 2200 MPa |
| Notched IZOD Impact | ASTM D256 | 150 J/m |
| Density | ASTM D256 | 1.19g/cm3 |