PC-50S

Source    CD      ，Application    Electronics、Optical

Performance table

|  | Testing standards |  |
| --- | --- | --- |
| Melt Flow Index | ASTM D1238 | 60-70 g/10min |
| Tensile strength | ASTM D638 | 55 MPa |
| Elongation | ASTM D638 | 40 % |
| Bending strength | ASTM D790 | 85 MPa |
| Bending modulus | ASTM D790 | 2100 MPa |
| Notched IZOD Impact | ASTM D256 | 100 J/m |
| Density | ASTM D256 | 1.19g/cm3 |