PCRGA-WB

Source    Water bottle       ，

Application   Electronics, Automotive

Performance table

|  | Testing standards |  |
| --- | --- | --- |
| Melt Flow Index | ASTM D1238 | 6-10 g/10min |
| Tensile strength | ASTM D638 | 65 MPa |
| Elongation | ASTM D638 | 110 % |
| Bending strength | ASTM D790 | 90 MPa |
| Bending modulus | ASTM D790 | 2250 MPa |
| Notched IZOD Impact | ASTM D256 | 850J/m |
| Density | ASTM D256 | 1.19g/cm3 |